## Slide 1
Lime-clast reservoirs and crack sealing
Hot mixing with quicklime
Modern mortar section (lime-clast specimen)
Hydraulic response (after flow exposure)
+
+
Quicklime
(CaO)
Siliceous
materials
Water
Fresh mortar with lime clasts
Calcium-rich
core
Si/Al-rich
rim
Ancient mortar (section)
Mechanistic
interpretation
Water ingress
(through crack)
Cement matrix
(with fine grains)
Porous lime clast
(Ca-rich reservoir)
Calcite precipitation
Pores
Ca²⁺
Ca²⁺
Carbonate supply
(from water)
Possible C-A-S-H
formation
Control
(no lime clasts)
Lime-clast specimen
(with lime clasts)
Open crack with
continuous flow
Calcite bridges narrow crack
Flow ceased in tested specimen
Tested gap: 0.5 ± 0.1 mm | 28-day cure | 2-month wet/dry preconditioning | Flow exposure: up to 30 days
Science Advances (2023) | doi:10.1126/sciadv.add1602 | Proposed mechanism; not to scale